## Slide 1
For the sensor …. Few times remove and insert
 Tin (Sn) plating
For the connector cable ….. Repeat using (remove and insert)
 Gold (Au) plating
Connector-pin plating …..
Gold plating is not really needed.
E2A passed all environmental test which fit to applications.

## Slide 2
Temperature change
Thermal expansion and contraction
Increase the resistance of a interface
Micro-motion of contactor pin
Fretting
at the connector interface
External vibration
Electromagnetic interactions
Connector fault
Wear away the plating surface
Oxidization film is formed
Mechanism of connector fault
Stock with high humidity
Cause (1)
Cause (2)
Cause (3)
Cause (4)

## Slide 3
Contact Resistance Test
 Less than 4m ohm
( at DC 20mV 20mA )
Judgment Criteria : less than 50m ohm
Insertion and Remove Force Test
Same level as Gold plating
Sensors are removed only few times.
Judgment Criteria : less than 40N
Enough level for sensors.

## Slide 4
High humidity test
Judgment Criteria : no-fault on basic specifications.
Heat cycle test
Judgment Criteria : no-fault on basic specifications.
Humidity : 75%
Temperature : 85 degrees C
72 hour
No fault by oxidization of the pin-plating
-40
85
deg. C
30min.
30min.
100 cycle
No fault by fretting movement
Vibration test
Judgment Criteria : no-fault on basic specifications.
External vibration :
frequency :10 to 2000 Hz
fluctuation : 1.5mm 15G
time : 15min. / sweep total 2.5 hours
No fault by fretting
( external vibration)