## Slide 1
Cable bending performance ……
E2A has the structure which protect the cable from bending.
(cable protector)
Cable can be bent at –40 degrees C atmosphere.

## Slide 2
Confidential
Bending times ( times）
Weight 500g
90 deg.
pulley
Cable bending test (at 23degC)
E2A keep same performance as E2EG.
It has the cable protector.
100000
50000
6.5
3.5
0.6
1.7
E2A
E2EG
IFM ＩＥＢ
All type
( dia. 4mm)
YAMATAKE
P+F N Ｊ１．５
0.6
Cable protector

## Slide 3
Test method
1) to wind the cable to rod by 6times.
Criterion
A crack should not be appeared on outer sheath.
Diameter of rod
= dia. 12mm
Sensor
Cable bending test at cold temp.
E2EG
( dia 4.0mm )
Temperature (deg.C)
0
-20
-40
E2A
All type
Improve the bending strength and the ease of wiring at low temperature.
The cable material was changed to softer.
Low temp. air
Release the winding
 Check the cable sheath.
Confidential
Cracked
at –45 deg.C
Cracked
at –25 deg.C
3) to release the cable winding.
2 hours
2) to put in the low temp. oven. 2.0 hours.