## Slide 1
Robot cable for E2A……
We can provide the special cable for cable bending application.
“Robot cable type”
“Robot cable type” has higher resistance for bending
Standard type : 65000 times  Robot cable type: 170000 times
e.g.

## Slide 2
Test result of “Robot cable type”
Weight 500g
90 deg.
pulley
Bending times ( times）
100000
50000
6.5
3.5
0.6
1.7
E2A
standard
E2EG
IFM ＩＥＢ
( dia. 4mm cable)
YAMATAKE
P+F N Ｊ１．５
0.6
150000
E2A
Robot
17
Normal breaking point of cable
Specifications of Robot cable
Cable protector + robot cable
(1) Special copper alloy metal for conductor
(2) Special PVC material which have higher strength for bending
Cost  approx. 0.7 Euro UP on standard cost / meter (cable length)

## Slide 3
Specifications of robot cable (1)
 | Items | Specifications
Conductor | Material | Copper alloy
 | Structure (number of strand) | 3/54/ dia0.05mm
 | Section | 0.318mm2
 | Outer diameter | Approx 0.83mm
Isolator | Material | Polyester elastomer (flame resisting)
 | Thickness | 0.25mm
 | Outer diameter | Approx 1.33mm
 | Color | Brown / Blue / Black
Outer sheath | Material | High elastic PVC
 | Thickness | 0.475mm
 | Outer diameter | 3.85mm
 | Color | Black
Outer sheath
Isolator
Conductor

## Slide 4
Specifications of robot cable (2)
 | Isolator | Outer sheath
Tensile strength (M Pa) | More than 18.0 | More than 9.8
Extend ratio (%) | 300.0 | 120.0
100% modulus (M Pa) | 18.0 | 3.8
Bending & Hot temp. | Not clack on the surface | 
Bending & Cold temp. | Not clack on the surface | 
Transformation ratio at 120degC (%) | Less than 1.5 | Less than 15.0
Cold temp. resistance (%) | -65.0 | -30.0
Hardness (HAD) | 98 | 78
(1) Lead (Pb) free (less than 100ppm)
(2) Mechanical characteristics
See 1)
See 3)
See 2)
1) Wind the cable to rod (dia. 12mm) 6 times  Keep in 120degC 1hour
2) Keep in –25 degC 1hour.  Wind the cable to rod (dia. 12mm) 6 times.
(2) Mechanical characteristics
(Selected data)