## Slide 1
Halogen Free cable for E2A
Now halogen free cable is available in E2A series.
Sep. 2005 OEE SenBU KT
Outer sheath = PUR
Insulator = TPE-E
thermoplastic elastomer ether ester block copolymer
This type can be realized by modification request.

## Slide 2
Structure of halogen free cable of E2A
E2A-*******-WH-**
TPE-E
PUR
Halogen free cable of E2A also has higher cable bending resistance.
10000 times bending (180deg 500g weight)
(DIN VDE 0472 Teil 603)
Sep. 2005 OEE SenBU KT

## Slide 3
Structure of halogen free cable type
Halogen free cable
Sep. 2005 OEE SenBU KT
Note) water proof level = IP67 (IEC 60947-5-2)
Same as standard type